**Description**

Suitable for hard surfaces, flexible non-porous or absorbing surfaces: marble, granite, painted cement, vinyl (PVC), linoleum and varnished parquet.

**Characteristics**

* Washable and anti-slip
* Protects and glosses without rubbing
* Easy to use
* Exceptional brightness, resistant to dirt and to acids
* For internal use
* Matt version available on request

**Composition**

Acrylic styrene copolymer, polyurethane and waxes. (APEOO-free)

**Preparation of surfaces**

Surfaces must be clean, dry, exempt of humidity and without traces of oils or fatty materials. We recommend carrying out a preliminary test.

**Application**

Agitate the container before use.

Apply a thin layer evenly and uniformly with suitable mohair cloth for wax. Without any use of force, a bright, shiny effect will appear. During the drying phase, do not polish any parts still drying.

After 2 or 3 hours you can apply a second coat if necessary.

For easy maintenance simply use a cloth moistened with our detergent **OL/MI01 Deterfloor**.

Wash tools with water after use.

**Consumption/Yield**

PROTECTION WAX has a yield of about 30 m²/lt per coat, depending on level of absorption and type of surface.

**Packaging and storage**

Plastic bottles of 1 lt and plastic cans of 5 lt. Stored in original, well-sealed containers, exempt from freezing or UV light, the product is stable for a period of 24 months. Store with a room temperature not below +5°C or above + 35°C. The product is sensitive to freezing.

**Health and safety regulations**

Ventilate during application.

Avoid contact with skin and eyes, in case of contact wash immediately with plenty of water.

Keep out of the reach of children.

As regards the evaluation of toxicological data, please see the safety data sheet.

**Disposal**

Dispose of the product according to local health and safety regulations. Empty containers must be recycled.

**Note**

Dolci colori srl reserves the right to modify this data sheet without prior notice.

Date: 19/08/19