Description

PITTURA THERMO-ISOLANTE is a matt, washable, water-based ecological paint for the decoration and protection of internal and external wall surfaces.

The particular characteristic of the product is its capacity to insulate in a more efficient manner than traditional paints available on the market.

The product has passed the tests:

ECOLABEL 3 and 4.

Characteristics

PITTURA THERMO-ISOLANTE combines thermal properties with an excellent permeability to water vapour and is completely washable. PITTURA THERMO-ISOLANTE respects the environment, has a very low level of volatile organic compounds (VOC) and conforms to the norm 2004/42/CE (D.Lgs. n.161 of 27th March 2006).

PITTURA THERMO-ISOLANTE does not contain volatile aromatic hydrocarbons (VAH).

Composition

Acrylic resins, water, methylcellulose, insulating agents, titanium dioxide, flower essences, calcium carbonate, wetting and dispersing agents, about 0.1% preservatives.

Surfaces

PITTURA THERMO-ISOLANTE can be applied on various types of surface such as plaster (cement, lime or mixed malta) lime-based plaster, cement, plaster, plasterboard, cement fibre and already painted surfaces.

The product should be applied on surfaces that are dry, non-flakey and exempt of salts and humidity.

Preparation of surfaces

On new surfaces, no pre-treatment is necessary; on already painted or damaged surfaces, it is necessary to remove the existing paint that presents problems of adhesion with the surface, fill any cracks with filler and apply a coat of ecological fixer Isofree IS/0245 diluted with water in the proportions of 1/7 or 1/8 to re-aggregate and uniform the surface.

If moulds or algae are present, treat the surface with Solu-zione ST PA/0800.

After having applied Isofree IS/0245 wait 6-8 hours before applying a first coat of PITTURA THERMO-ISOLANTE.

Application

Mix well before use.

This paint is generally diluted with about 10 – 20 % of water, according to the conditions of application, of the type of surface and the tools used.

Applied in two coats, the product is touch-dry after about 4-6 hours and completely dry after 24 hours.

Do not apply at a temperature below +5°C or above +35 with humidity >80%.

Wash tools with water after use.

Colours

Washable paint THERMO-ISOLANTE is white and thanks to the colouring system Imagine, Elements, Ral, Ncs it is possible to obtain over 1000 colours with our collection of universal colouring pastes, which are non-toxic and VOC exempt.

Warning

Protect doors, windows, frames and in general all parts that should not be painted. Any stains or splashes should be removed immediately with water.

Consumption

PITTURA THERMO-ISOLANTE has a yield of about 5 - 6 m²/lt per coat, depending on the level of absorption and type of surface.

Equipment for application

PITTURA THERMO-ISOLANTE can be applied by brush or roller.

Wash equipment with water after use.

Packaging and storage

Plastic buckets of 4 and 15 lt.

PITTURA THERMO-ISOLANTE should be stored in the original containers, well-sealed and is stable for at least 12 months, providing it is stored in a room at a temperature not below +5°C or above +30°C.

Health and safety regulations

Ventilate during application.

Avoid contact with skin and eyes, in case of contact wash immediately with plenty of water.

Keep out of the reach of children.

As regards the evaluation of toxicological data, please see    the safety data sheet.

Disposal

Dispose of the product according to local health and safety    regulations. Empty containers must be recycled.

Classification and technical characteristics

PITTURA VELVET has been tested at the GFC Chemical laboratory: the results of the tests reported in the tables below are documented in the test reports

n. 160L of 10.06.14.

Physical-chemical characteristics

| Description | Result |
| --- | --- |
| For final use | Decoration-protection |
| For type of chemical binder | Paint with acrylic binder |
| For the state of solution or dispersion of the binder | Dispersion soluble in water |
| Specific weight | 0.96 ± 0.05 gr/ml |
| Viscosity | 9000-13000 cPs |
| pH | 8-10 |

Technical characteristics

| Description | Norm | Result |
| --- | --- | --- |
| Permeability to vapour | UNI EN ISO 7783 | Sd = 0,1583 m Thickness = 668(m (= 176 |
| Content of VOC | -Criteria n° 3 and n° 4 Ecolabel (Decision of the Commission of the European Community 2009/544/CE and Norm ISO 11890-2:2006) -D.Lgs. n.161 of 27/03/2006 and directive 2004/42/CE | 0.82 gr/lt |
| Content of VAH | Criteria n° 3 and n° 4 Ecolabel (Decision of the Commission of the Eurpean Community 2009/544/CE and Norm ISO 11890-2:2006) | Absent |

Thermal insulation. Insulating paint (black curve) compared to traditional paint (red curve)

Date : 11/11/19