**Description**

UNIVERSAL PAINT STRIPPER is an organic-solvents-based and dicloromethane-free product. It appears as a pasty product with such a viscosity that makes it possible for it to be applicable both on horizontal and vertical surfaces.

**Characteristics**

Perfect on synthetic, oil and nitrocellulose-based paints, as well as on acrylic, polyester, polyurethane-based varnishes, cold and oven enamel, wall water-based paints, plasters and glues for carpets and wood floorings.

.

**Surfaces**

If used on wood, being a natural and non-uniform surface, we advise to make a test on a small and not too visible area in order to avoid undesirable effects.

Avoid use on plastic materials as well as on surfaces exposed to heat or sun.

PRODUCT NOT SUITABLE FOR CAR BODIES

**Instructions for use**

Ready for use, do not dilute.

Stir well after opening.

Apply abundantly a coat of SVERNICIATORE UNIVERSALE | UNIVERSAL PAINT STRIPPER with a brush, a putty knife or a sponge and wait until the product is fully absorbed .

For polyester varnishes and oven enamels 4-10 hours are needed.

For polyurethane-based ones 1-2 hours.

For synthetic paints 10-20 minutes.

Proceed afterwards with a putty knife, a cloth or a jet of water to remove the paint.

Allow 24 hours for drying before applying a new finishing.

**Consumption**

The yield depends on various factors, such as :

* temperature of the environment ;
* number of layers to remove ;
* type of varnish (polyester, polyurethane, synthetic) ;
* type of surface.

Treatable surface : around 2 m²/litre

**Packaging and storage**

UNIVERSAL PAINT STRIPPER is packaged in metal jars with a 0,75 l. capacity.

The product preserved in its original package, and kept in a fresh environment and not exposed to frost and UV rays, remains unaltered for at least 24 months.

Keep the product at temperatures between +5°e +30° C. The product does not tolerate frost.

**Health and safety regulations**

Avoid contact with any plastic material and application on hot or UV rays-exposed surfaces.

Do not stir before use.

Open the lid with particular attention as the product could produce sudden spurts if exposed to pressure; successively cover the mouthpiece with a cloth and pull the opening ring slowly until the air is expelled, always keeping the product at a safe distance from the face.

Keep the container well closed, away from any source of heat and in a fresh and dry environment.

We decline any responsibility for damage caused if the product is handled in disregard of the above mentioned safety precautions.

For further information, please refer to the safety sheet.

Ventilate during application.

Avoid contact with skin and eyes, in case of contact wash immediately with plenty of water.

Keep out of the reach of children.

As regards the evaluation of toxicological data, please see the safety data sheet.

**Disposal**

Dispose of the product according to local health and safety regulations. Empty containers must be recycled.

Date : 11/11/19